## Slide 1: Equilibrium Analysis 2 CO → CO2 + C
Suppose a gas mixture of 3 moles of CO and 2 moles of CO2 is held at 800 ºC and 1 atm. Determine whether graphite can form according to the reaction above, and if so, calculate the equilibrium ratio of CO to CO2. Note that at 800 ºC the free energies of formation of CO and CO2 are -182.5, and -395.6 kJ mol-1, respectively, and the free energy of formation of graphite is 0 kJ mol-1.

## Slide 2: Solution
Write the equilibrium expression
Calculate the equilibrium constant
Express activities in terms of composition
Express composition in terms of extent of reaction
Solve for extent
Calculate final composition
Notes: These are the steps involved in solving this problem

## Slide 3: The Equilibrium Expression
Notes: Note: The activity of the solid, graphite is equal to 1.
Will show where the value of K came from on next slide.
Assumed ideal gases to convert activities to moles, then used mole table to convert to extent

## Slide 4: The Equilibrium Constant
Usually need to calculate K(298K), generate an expression for ∆H(298K), integrate within equation (4.6), etc.
  That’s because generally only K(298K) can be calculated directly
Here, have ∆G of formation data at 1073 K, so K(1073K) can be calculated directly

## Slide 5: Point to Note
In some situations, you may not know whether or not a solid phase will exist when the system reaches equilibrium
  If it does not, then the reactions involving the solid phase don’t actually take place and they should not have been included in the analysis
    Because they were included in the analysis, the results of the analysis will not make sense on physical grounds
  Since you don’t know before the fact, you assume that they do take place and write the equilibrium expressions for them
    If you then proceed to calculate a meaningful final equilibrium composition, this assumption was valid
    If instead you calculate a final equilibrium composition that does not make physical sense, this indicates that the reaction does not take place and should not have been included in the analysis (of course you need to make sure that you didn’t make other errors while performing the calculation)

## Slide 6: Another Point to Note
The method given in Unit 3 for calculating an equilibrium constant at some temperature T involves calculating the equilibrium constant at 298 K and integrating a function of the heat of reaction from 298 K to T
  This assumes that free energy data are only available at 298 K
  If free energy data are available at the temperature T, then the equilibrium constant can be calculated directly as was done in this activity